ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC144 | Institute: University of Chicago |
| --- | --- |

| CONTROL | Data | Comments |
| --- | --- | --- |
| Date of the stacking | September 27, 2000 |  |
| Date of final welding | September 29, 2000 |  |
| Date of surface protection | October 11, 2000 |  |
| Coil identification: masters | Pallet #88, 32 plates |  |
| Box identification: spacers | 5/13-13 |  |
| Glue batch number | Hardener 20590303 Resin 20592103 |  |
| Glue drop size – start (gm) | 0.1462 | at 10:10 |
| Glue drop size – middle (gm) | 0.15475 | at 11:50 |
| Glue drop size – end (gm) | 0.1495 | at 13:10 |
| Stacking time (h:m) | 3:10 |  |
| Gluing curing time ( h:m) | 45:00 | Clamp at 13:30 Unclamped at 10:40 on Sept. 29 |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Tracy Westmoreland |  |
| Final Welding: Welder name | Tracy Westmoreland |  |
| Weld inspection (OK/NOK) | OK |  |
| Observations: Spacer shims at slots II, III, IV, V, XI, and I. Key shim was increased from 0.007” to 0.008”. |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 12-99

Last date of welder qualification (final weld)	: 7-00

Quality Control Leader: Kelby Anderson, Elizabeth Pod Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC144 | Institute: University of Chicago |
| --- | --- |

# THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

# SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.64 | 292.05 | 292.13 | 292.21 | 292.04 | 291.81 | 291.61 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.60 | 291.81 | 291.98 | 292.18 | 292.10 | 292.11 | 291.61 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.63 | 291.93 | 292.04 | 292.07 | 292.04 | 291.93 |

# Maximum deviation from nominal (+): 292.21; 0.51

# Maximum deviation from nominal (-): 291.60; 0.10

Quality Control Technician (Print): Elizabeth Pod Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC144 | Institute: University of Chicago |
| --- | --- |

# Feeler Gauge Measurements

# Narrow End:

# Left Side:				Right Side:

| Top | N/A | N/A |
| --- | --- | --- |
| 5.75” | N/A | N/A |
| Bottom | N/A | N/A |

# Section 1:

# (.5” from weld area on narrow end)

# Left Side:				Right Side:

| Top | N/A | N/A |
| --- | --- | --- |
| 5.75” | N/A | N/A |
| Bottom | N/A | N/A |

* 5.75” refers to 5.75” from bottom

Observations/Drawings:

Quality Control Technician (Print): N/A Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC144 | Institute: University of Chicago |
| --- | --- |

# SUBMODULE GLUEING, INSPECTION & CLEANOUT

Gluing

Resin identification: 20592103 			 Hardener identification: 20590303

Dosage control (gm/point). (Final range to be determined from glue system qualification)

# Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| Pre-Stacking (gm/point) | 0.1462 |  |  |  |  | 0.1462 |
| Post-Stacking (gm/point) | 0.1462 | 0.1495 |  |  |  | 0.1502 |

Pre-Cleanout Inspection

# Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 7 | 2 | 1 | 1 | 0 | 2 | 0 | 0 | 1 | 2 | 13 |

Post-Cleanout Inspection

# Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

# Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Elizabeth Pod Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC144 | Institute: University of Chicago |
| --- | --- |

# FINAL WELDING

# Date of Welding: September 29, 2000

# Welding Filler Rod Material: ER70S-2

# Weld Inspection (as defined in technical specification) – OK/NOK: OK

# 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

# 2.	No Cracks

# 3.	Thorough fusion

# 4.	All craters filled to full cross section

# 5.	Undercut does not exceed .25mm

# 6.	No visible porosity

# 7.	Weld profile conformance

# Note any required repairs:

# Note any variances from technical specification:

Weld procedure was completed to narrow end of module as follows: 3” weld on 6” centers.  Allowed to completely cool until almost no warmth could be felt in the weld zone.  Repeated until weld is completed.

# Comments:

Welder Name (Print): Tracy Westmoreland Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC144 | Institute: University of Chicago |
| --- | --- |

# SURFACE PROTECTION

# Date of Surface protection: October 11, 2000

# Paint batch and production date:

Batch number: 0199 20

Production Date: 14 Vil 1999

# Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 15 |

# Control of Paint Flow

# Energy velocity, as specified in general QC procedures note.

# Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 42.04 sec/ 6cm | 42.04 sec/ 6cm | 42.04 sec/ 6cm |

Calculations:

171.25cm /X minutes ( Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes ( 6cm/Z minutes

X= 20

Y= 8.5625

Z= 0.7007 ( 42.04 seconds/ 6 cm

# Visual Inspection (OK/NOK): OK

# Comments:

Mixed paint to 15 seconds.  Started to fill the hopper at 9:15 at 40 PSI and inserted the submodule at 9:35.  It was totally submerged at 9:40.  Started emptying procedures at 10:10 at 40 PSI and finished at 10:30.  The submodule was horizontal at 10:50.

Quality Control Technician (Print): Greg Wilkins Date: Signature: