# ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC045 | Institute: University of Chicago |
| --- | --- |

| CONTROL | Data | Comments |
| --- | --- | --- |
| Date of the stacking | September 3, 1999 |  |
| Date of final welding | September 30, 1999 |  |
| Date of surface protection | January 20, 2000 | Greg Wilkins |
| Coil identification: masters | Pallet #02 |  |
| Box identification: spacers | 11-15/13 |  |
| Glue batch number | Hardener 20405183 Resin 20392483 |  |
| Glue drop size – start (gm) | .1665 |  |
| Glue drop size – middle (gm) | .1726 |  |
| Glue drop size – end (gm) | .1247 |  |
| Stacking time (h:m) | 3:05 |  |
| Gluing curing time ( h:m) | N /A |  |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Cindy Dyrda | UCEC |
| Final Welding: Welder name | Cindy Dyrda | UCEC |
| Weld inspection (OK/NOK) | OK |  |
| Observations: | Shim 0.015 inches, central part only, no shim on ends |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: 7-99

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC045 | Institute: University of Chicago |
| --- | --- |

# THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

# SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.58 | 291.16 | 291.23 | 291.15 | 290.88 | 291.23 | 290.65 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.53 | 291.07 | 291.16 | 291.03 | 291.84 | 291.05 | 290.51 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.56 | 291.11 | 291.20 | 291.09 | 290.85 | 291.18 |

# Maximum deviation from nominal (+): 291.84, .14

# Maximum deviation from nominal (-): 290.51, 1.19

Quality Control Technician (Print): Marva Maya Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC045 | Institute: University of Chicago |
| --- | --- |

# Feeler Gauge Measurements

# Narrow End:

# Left Side:				Right Side:

| Top | 0.0 | 0.0 |
| --- | --- | --- |
| 5.75” | 0.014 | 0.005 |
| Bottom | 0.014 | 0.005 |

# Section 1:

# (.5” from weld area on narrow end)

# Left Side:				Right Side:

| Top | 0.002 | 0.006 |
| --- | --- | --- |
| 5.75” | 0.005 | 0.004 |
| Bottom | 0.0 | 0.005 |

* 5.75” refers to 5.75” from bottom

Quality Control Technician (Print): Marva Maya Date: October1,1999 Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC045 | Institute: University of Chicago |
| --- | --- |

# SUBMODULE GLUEING, INSPECTION & CLEANOUT

Gluing

Resin identification: 20392483 			 Hardener identification: 20405183

Dosage control (gm/point). (Final range to be determined from glue system qualification)

# Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| Pre-Stacking (gm/point) | .1665 |  |  |  |  | .1665 |
| Post-Stacking (gm/point) | .1665 | .1726 | .1747 |  |  | .1713 |

Pre-Cleanout Inspection

# Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | All | 2 | 1 | 2 | 1 | 0 | 0 | 0 | All | All | All |

Post-Cleanout Inspection

# Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

# Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK					Small keys (OK/NOK): OK

Quality Control Technician (Print): Lex Mills Date: January 18, 2000 Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC045 | Institute: University of Chicago |
| --- | --- |

# FINAL WELDING

# Date of Welding: September 30, 1999

# Welding Filler Rod Material: ER70S-2

# Weld Inspection (as defined in technical specification) – OK/NOK: OK

# 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

# 2.	No Cracks

# 3.	Thorough fusion

# 4.	All craters filled to full cross section

# 5.	Undercut does not exceed .25mm

# 6.	No visible porosity

# 7.	Weld profile conformance

# Note any required repairs:

# Note any variances from technical specification:

Weld procedure was completed to narrow end of module as follows: 3” weld on 6” centers.  Allowed to cool until almost no warmth could be felt in the weld zone.  Repeated until weld is completed.

# Comments:

Welder Name (Print): Cindy Dyrda Date: Sepetmber 30, 1999 Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC045 | Institute: University of Chicago |
| --- | --- |

# SURFACE PROTECTION

# Date of Surface protection: January 20, 2000

# Paint batch and production date:

Batch Number: 0199 20

Production Date: 14VIL 1999

# Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 20 |

# Control of Paint Flow

# Energy velocity, as specified in general QC procedures note.

# Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 63.06sec/6cm | 63.06sec/6cm | 63.06sec/6cm |

Calculations:

171.25cm /X minutes ( Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes ( 6cm/Z minutes

X= 30minutes

Y= 5.7083333 cm/minutes ( 5.709 cm/minute

Z= 1.051 minutes ( 63.06 seconds

# Visual Inspection (OK/NOK): OK

# Comments:

Start to fill at 12:10 at 40 PSI. The submodule was inserted at 12:45and submerged at 12:50. Start emptying at13: 30 at 40 PSI and finished at 14:00.  The submodule was horizontal at 14:45.

Quality Control Technician (Print): Greg Wilkins Date: Signature: