## Slide 1
Quantum Effects in Electron Emission from Nanodiamond
Sergey Baryshev
Electrical and Computer Engineering
Michigan State University
Center for Bright Beams, University of Chicago
Monday, June 3, 2019
https://www.egr.msu.edu/mam/

## Slide 2
Acknowledgments
Dr. Stas Baturin
U Chicago
Prof. Andreas Schroeder @ UIC
Dr. Alexander Zinovev @ ANL
Gongxiaohui Chen
co-advisee @ Illinois Tech
Tanvi Nikhar
PhD @ ECE, MSU
Dr. Oksana Chubenko
ASU

## Slide 3
Some background
Solid state
Surface science
Accelerator R&D

## Slide 4
ASET program at PA/ECE, MSU
On September 25, 2017, the U.S. Department of Energy Office of Science Office of High Energy Physics awarded MSU a five-year Accelerator Science and Engineering Traineeship (ASET) cooperative agreement to train domestic graduate students in four areas of emphasis to meet future workforce
*offers full 2 year support at MSU followed by PhD research at U.S. Nat’l Labs
Physics of large accelerators and systems engineering
Superconducting radiofrequency accelerator physics and engineering
Radiofrequency power system engineering
Cryogenic systems engineering (especially liquid helium systems)
Peter Ostroumov and Steve Lund are PI’s from Physics and Astronomy
*ASET is tightly related with USPAS and Nuclear Physics program (#1 in US)
John Verboncoeur is co-PI from ECE

## Slide 5
Talk outline
~ Quantum efficiency and mean transverse energy of nanodiamond photocathode
~ Electron emission saturation effect of nanodiamond field emitter
~ Light emission and self-heating of nanodiamond field emitter

## Slide 6
Excellent solar blind photocathode QE>~1-10%
Proc. SPIE 4139, 16 (2000)
PRB 20, 624 (1979)
CBM
Diamond is a NEA material
Single crystal
Poly crystal

## Slide 7
Nano- and ultra-nano- crystalline diamond: what’s in a name?
Microcrystalline:
dia. grain ≥500 nm
Nanocrystalline:
dia. grain 10-200 nm
UNCD:
dia. grain ≤10 nm
MRS Bulletin 35, 281 (2010)

## Slide 8
Importance of grain boundaries
Field- and photo- emission data is consistent:
sp2 grain boundaries (GBs) emit electrons
PRB 60, 16135 (1999);Carbon 94, 386 (2015)
Electron transport is also through sp2 GBs:
m* ≈ 1/18m0
PRB 82, 184206 (2010)

## Slide 9
The ideal cathode not only would have high QE and low emittance, but it should also help mitigate image and space charge forces by emitting electrons with a high average velocity
Ref: Dowell’s summary @ P3 2014
Single crystal vs. polycrystalline diamond
CVD single crystal
upward band bending
CVD ultrananocrystalline
no bending
add
barrier
~2 eV

## Slide 10
N-incorporated UNCD field emitters: no sharp needles
(N)UNCD:
grain ≤10 nm
Proc. SPIE 7679, 76791N (2010)
Excellent field emitter: low turn on field, high charge

## Slide 11
Nanodiamond
photocathode

## Slide 12
Effective work function is activation energy of a dopant!
x
E
εg≈5.5 eV
N: εa≈1.7 eV
P: εa≈0.6 eV
S: εa≈0.4 eV
VBM
CBM
H
C
χ≈–1 eV
Vacuum level
surface
Naive picture of diamond doping

## Slide 13
(N)UNCD / Basic characterization
Microwave-assisted plasma chemical vapor deposition
100-200 nm highly conductive (N)UNCD by SEM and Raman

## Slide 14
A
V
Light in
e– out
KP tip
(N)UNCD:H samples transfer: 2 hours in air
Pérez Quintero et al., APL 105, 123103 (2014)

## Slide 15
Experimental results on work function and QE
Work function drops after H-termination!
QE substantially grows!
Pérez Quintero et al., APL 105, 123103 (2014)

## Slide 16
MTE experiment at UIC
I=1.83 A,
focus on YAG screen
Berger and Schroeder, JAP 108, 124905 (2010)

## Slide 17
MTE results and why are they so?
Chen et al., APL 114, 093103 (2019)
266 eV
DS 1/3 line
checked by
Karkare and Bazarov,
PR Appl. 4, 024015 (2015)
roughness ~10 nm
No phys or chem roughness effects
says (N)UNCD:H could be x100 brighter than Cu

## Slide 18
No effective mass effect
Expected value would be 30 meV from transverse momentum pT conservation
but we measure ~300 meV
Classical metal (m* = m0)
pT,max=(2m0(ħω – ))1/2 = (2m0ΔE)1/2
Metal with m* < m0
pT,max=(2m0ΔE)1/2 > (2m*EF)1/2
Chen et al., APL 114, 093103 (2019)
Vacuum level
PRL 111, 237401 (2013)

## Slide 19
Working hypothesis:
ground state spatially confined photoemission
Tanvi’s work in progress with
Fraunhofer Diamond Center and UIC
The Uncertainty Principle
ΔxΔpT≥ħ/2
tells us
266 meV  1 nm (GB size!)
Chen et al., APL 114, 093103 (2019)
Chubenko et al., JAP 125, 205303 (2019)

## Slide 20
Graphitic patch model and optimal (N)UNCD:H design
NEA induced on diamond grains (χ≈–1 eV)
around sp2 GB lowers their work function by 1 eV Ref: PRB 60, 16135 (1999)
In balanced (N)UNCD (balanced sp3-to-sp2 ratio of ~1/10) we may get the best of all worlds:
~ GB large enough  low MTE, 50-100 meV;
~ GB crystallized well  0.1 Ω×cm for good electron supply  no image charge;
~ Large sp2 fraction  good overlap between π and π*, π* is 1-2 eV below the diamond conduction band minimum/vacuum level  low emission threshold (can be in the visible);
~ Emission from well crystallized graphitic  ultrafast emission

## Slide 21
Saturation

## Slide 22
plasma/
breakdown
p- type Ge
Arthur, JAP 36, 3221 (1965)
Phys. Stat. Solidi B 1700268 (2017)
metallic CNT
semicond CNT
Deviation from FN law in nonmetals (saturation)
JVSTB 31, 02B101 (2013);
IVNC S9-C1 (2014)
n-Si
p-Si

## Slide 23
Semi-metallic (N)UNCD also saturates!
Chubenko et al., ACS Appl. Mater. Interfaces 9, 33229 (2017)

## Slide 24
Field emission projection microscope
Baturin and Baryshev, Rev. Sci. Instrum. 88, 033701 (2017)
(a)

## Slide 25
What’s going on (N)UNCD surface?
Field of view is 4.4 mm

## Slide 26
3 different samples and 4 lessons
~ Semi-metallic (N)UNCD saturates similarly to semiconductors
~ In planar uniform (N)UNCD, field emission is not uniform
~ Emission area depends on electric field
~ Saturation is ~100 mA/cm2 is specific to (N)UNCD, regardless of substrate
Chubenko et al., ACS Appl. Mater. Interfaces 9, 33229 (2017)

## Slide 27
Chubenko et al., JAP 125, 205303 (2019)
Band diagrams

## Slide 28
Stratton–Baskin–Lvov–Fursey formalism
Stratton, Proc. Phys. Soc. B 68, 746 (1955) and Phys. Rev. 125, 67 (1962)
Baskin, Lvov, Fursey, Phys. Stat. Solidi B 47, 49 (1971)
Poisson
Stratton
Chubenko et al., JAP 125, 205303 (2019)

## Slide 29
Describing saturation: theory vs. experiment
image process
266 meV  0.9
Child-Langmuir
Chubenko et al., JAP 125, 205303 (2019)

## Slide 30
Saturation: diode-to-resistor switching
rFN= ∂V/∂I
(∞→0)
rS= ∂V/∂I
(0→large N)
+
JVSTB 31, 02B101 (2013);
IVNC S9-C1 (2014)
n-Si
p-Si

## Slide 31
Baturin et al., arXiv:1710.03692 (2017)
General series resistor formulas
emission term
supply term
v∞ ~107 cm/s
limited!

## Slide 32
Formulas versus experiments
single tip p-Si
arrayed n-Si
single CNT
fiber CNT
planar (N)UNCD
I, A
E, V/cm
JVSTB
31, 02B101 (2013)
IVNC S9-C1 (2014)
Nano Lett. 5, 2135 (2005)
APL 105, 173107 (2014)
Chubenko et al., ACS Appl. Mater. Interfaces 9, 33229 (2017)

## Slide 33
Any relevance to photocathodes?
Quick depletion in photocathodes based on 2D materials/2D surface states?

## Slide 34
Heating, evaporation
and blow away

## Slide 35
Blue light from (N)UNCD
ITO
YAG
SEM

## Slide 36
First evidence for micro-plasma formation
Side-view into the gap
Current vs. time
Pressure vs. time

## Slide 37
sp2 content of UNCD versus emissivity
All samples
~100 μA@1 kV
Baturin et al., J. Phys. D: Appl. Phys. 52, doi:10.1088/1361-6463/ab2183 (2019)

## Slide 38
Side-view (in gap) and front-view (on YAG)
Vacuum ~10-9 Torr
Front-view
Side-view
Baturin et al., J. Phys. D: Appl. Phys. 52, doi:10.1088/1361-6463/ab2183 (2019)

## Slide 39
Self-induced, self-stabilized glow discharge

## Slide 40
Two estimations on temperature
Phase diagram
(T>~3,500 K)
Diamond-to-graphite
(T>~2,000 K)
Baturin et al., J. Phys. D: Appl. Phys. 52, doi:10.1088/1361-6463/ab2183 (2019)

## Slide 41
Third temperature estimation
unstable 4,500 K
(meff~1/18m)
stable 2,000 K
(meff~1/2m)

## Slide 42
In situ light emission and breakdown formation
PR Rev. Accel. Beams 21, 122002(2018)
1500 K

## Slide 43
Any relevance to photocathodes?
Nottingham-like heating in low mass photocathodes?